## Slide 1: Electron Pairing and Superconductivity in SrTiO3-based Nanostructures and Waveguides
Jeremy Levy
Pittsburgh Quantum Institute
Department of Physics and Astronomy University of Pittsburgh
Nordita Program on Multi-Component and Strongly-Correlated Superconductors Stockholm, Sweden 4 July 2016
Notes: Electron Pairing and Superconductivity SrTiO3-based Nanostructures and Waveguides
The study of strongly correlated electronic systems and the development of quantum transport in nanoelectronic devices have followed distinct, mostly non-overlapping paths. Electronic correlations of complex materials lead to emergent properties such as superconductivity, magnetism, and Mott insulator phases. Nanoelectronics generally starts with far simpler materials (e.g., carbon-based or semiconductors) and derives functionality from doping and spatial confinement to two or fewer spatial dimensions. In the last decade, these two fields have begun to overlap. The development of new growth techniques for complex oxides have enabled new families of heterostructures which can be electrostatically gated between insulating, ferromagnetic, conducting and superconducting phases. We use a scanning probe to “write” and “erase” conducting nanostructures at the buried LaAlO3/SrTiO3 interface with a precision of two nanometers. Using this technique, we investigate the phenomenon of electron pairing in SrTiO3. Low-temperature measurements of sketched single-electron transistors reveal clear signatures of electron pairing, far outside the regime of temperatures and magnetic fields that permit them to become phase coherent and superconducting. Electron pairing without superconductivity is also observed in open ballistic quantum wires that exhibit quantized conductance. An understanding of electron pairing in SrTiO3-based nanostructures creates new constraints for theory, and raises the prospect that an unconventional “high-temperature” (relative to carrier density) superconductor may be deeply understood.

## Slide 2: Acknowledgements
Mengchen Huang Shicheng Lu Jeremy Levy Guanglei Cheng Michelle Tomczyk Patrick Irvin
Joshua P. Veazey
Anil Annadi
Megan Kirkendall
Anthony Tylan-Tyler
David Pekker
U. Pittsburgh
Andrew Daley
Alexander
Tacla
U. Strathclyde
C. Stephen Hellberg
NRL
Chang-Beom
Eom
Hyungwoo
Lee
Sangwoo
Ryu
U. Wisconsin-Madison

## Slide 3: Correlated Nanoelectronics
Combine the rich phenomena of correlated oxides with the paradigm of semiconductor nanostructures
Correlated Oxides: superconductivity, magnetism, ferroelectricity, ferroelasticity,…
Semiconductor nanoelectronics: Quantum transport, single electron charge/spin devices,…
http://www.weizmann.ac.il/condmat/imry/content/images-selected-nano-systems
Complex oxides add richness to mesoscopic devices
Mesocopic devices reveal properties of oxides

## Slide 4: Oxide Yatzhee
SrTiO3
Edition!
oxide
“The complexities of the crystal structure, lattice waves, band structure, transport properties, impurity electrons and superconductivity have inspired the comment: ‘if SrTiO3 had magnetic properties, a complete study of this material would require a thorough knowledge of all of solid state physics.’”
--Marvin L. Cohen, in Superconductivity, vol. 1, R. D. Parks, Ed. (New York, 1969).

## Slide 5: Emergent Phenomena at Oxide Interfaces
High-mobility 2DEG
  Ohtomo and Hwang, Nature (2004)
Metal-insulator transition
  Thiel et al, Science (2006)
Superconductivity
  Reyren et al, Science (2007); Caviglia, Nature (2008)
Magnetism
  Brinkman et al, Nature Materials (2007)
Tunable Spin-Orbit Coupling
  Caviglia et al, PRL. (2010); Ben Shalom et al, PRL (2010)
Nanostructures
  Cen et al, Nature Materials (2008)
Nanodevices
  Cen et al, Science (2009)
Notes: Emilio Artacho gave a nice introduction on Wednesday.

## Slide 6
Interface <3 unit cells LaAlO3 is insulating
Interface >3 unit cells LaAlO3 is conducting
Interface =3 unit cells LaAlO3 can switch!

## Slide 7
Interface <3 unit cells LaAlO3 is insulating
Interface >3 unit cells LaAlO3 is conducting
Interface =3 unit cells LaAlO3 can switch!

## Slide 8
Interface <3 unit cells LaAlO3 is insulating
Interface >3 unit cells LaAlO3 is conducting
Interface =3 unit cells LaAlO3 can switch!
insulating
conducting

## Slide 9: Etch-a-Sketch Nanoelectronics
Toy
Tool

## Slide 10: LaAlO3/SrTiO3 Nanostructures
SrTiO3
LaAlO3
Ti/Au
interface
contact
Conductive AFM tip
Vtip
Vtip>0 writes
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
protons
-
-
-
-
-
-
electrons
≥ 2 nm
n ~ 1013 cm-2
barrier
1.2 nm
Vtip<0 erases
Vtip=3 V
C. Cen et al, Nature Materials 7, 298 (2008). C. Cen et al, Science 323, 1026 (2009)

## Slide 11: Oxide Nanoelectronics On Demand
SketchFET Transistors
Cen et al., Science 6, 343 (2009)
Nanoscale Diodes
Bogorin et al., APL 97, 013102 (2010)
Anomalous High Mobility @ RT
Irvin et al., Nano Letters 13, 364 (2013)
Multiple Tip Lithography
Li et al., IEEE Trans. Nano. 12, 518 (2013)
Molecular-Scale THz Spectroscopy
Ma et al., Nano Lett 13, 2884 (2013) Jnawali et al., APL 106, 211101 (2015)
Nanoscale Photodetector
Irvin et al, Nature Photonics 4, 849 (2010)

## Slide 12: Oxide Nanoelectronics On Demand
Single Electron Transistor
Cheng et al, Nature Nano 6, 343 (2011)
Nonlocal Transport
Cheng et al, PRX 3, 011021 (2013)
Veazey et al, EPL 103, 57001 (2013)
Electron Pairing without Superconductivity
Cheng et al, Nature 521, 196 (2015)
Reconfigurable Superconducting Nanoelectronics
Veazey et al, Nanotechnology 24, 375201 (2013)
Graphene-Complex Oxide Heterostructures
Huang et al, APL Materials 3, 062502 (2015)
Electronically Controlled Ferromagnetism @ RT
Bi et al, Nature Communications 5, 5019 (2014)

## Slide 13: Electron Pairing Without Superconductivity
Nature 521, 196 (2015)

## Slide 14: Electron-Electron Interactions
Attractive interactions (U<0) lead to electron pairing and superconductivity
Repulsive interactions (U>0) associated with Mott insulator, Wigner crystal (and possibly high-Tc SC)
Strategy: probe electron-electron interactions in LAO/STO quantum dot
U<0
U>0

## Slide 15: SrTiO3: The First Superconducting Semiconductor

## Slide 16
“…the non-monotonic temperature dependence bears a striking resemblance to high temperature superconductors—which will be discovered twenty years from now.”

## Slide 17
BEC-BCS Crossover
Notes: David M. Eagles

## Slide 18: Fast-forward to the present…

## Slide 19: Pseudogap phase in LAO/STO
Nature 502, 528–531 (2013)

## Slide 20: SrTiO3 Single-Electron Transistor
Mesocopic devices reveal properties of oxides

## Slide 21: Transport in a single-electron transistor (SET)
Conductance
Vgate
Ec+ε
Ec
µd
µs
Ec
Ec+ε
Ec = Coulomb energy
e = orbital energy
Vsd
Vgate
Resonant Tunneling
Energy “Ladder”
Single-electron transistor
Cheng et al, Nature 521, 196 (2015)

## Slide 22: Magnetic field dependence in a SET
Single particle energy levels
Vsd
Vsg
Finite B
B=0
Non-zeroB
Vsg
B
Ec
E
ε
Vsd
Vsg
B=0 T
Ec+ε
Ec
Cheng et al, Nature 521, 196 (2015)

## Slide 23: Device schematic and transport characteristics
Low electron density High electron density
w=5 nm
T=50 mK
Cheng et al, Nature 521, 196 (2015)
Notes: In transport, we see diamonds-shaped regions of no conductance, but in a field, instead of just changing size, we see a doubling of the diamonds. If we look at the positions of the conductance peaks as a function of the magnetic field, we see that at low fields, the peak spacing is insensitive to field, then at some finite critical field, the peaks begin to split.

## Slide 24: Emergence of new diamonds
0T
1T
2T
3T
4T
T=50 mK
Cheng et al, Nature 521, 196 (2015)
Notes: Let’s briefly take a closer look at what these splittings mean for transport. At zero field here we see three diamonds and two peaks. The two peaks begin to broaden at 2T, and by 3T we see that each peak has begun to split, with small islands emerging between them. By 4T these islands have grown into new diamonds.

## Slide 25: Emergence of new diamonds
Doubly-degenerate resonances—electron pairs
Pairs split above B=2 Tesla
Zero-bias
conductance
Cheng et al, Nature 521, 196 (2015)
Notes: Let’s briefly take a closer look at what these splittings mean for transport. At zero field here we see three diamonds and two peaks. The two peaks begin to broaden at 2T, and by 3T we see that each peak has begun to split, with small islands emerging between them. By 4T these islands have grown into new diamonds.

## Slide 26: Electron Pairing Transition
Below Bp
  Electrons paired
  No Zeeman shift
Above Bp
  Zeeman splitting
Pairing temperature in range 1-10 Kelvin
Pairing field is 10x larger than Hc2/mB
superconducting
Cheng et al, Nature 521, 196 (2015)

## Slide 27: Attractive Hubbard Model
t=1 meV
U=-0.8 meV
Theory
negative
Experiment
Cheng et al, Nature 521, 196 (2015)

## Slide 28: Electron Pair Generation Gap
T=50 mK
Cheng et al, Nature 521, 196 (2015)
Three distinct electronic phases

## Slide 29
Previously realized only in ultracold atomic gases
Strong pairing mechanism still not understood
  Bipolarons?
  Negative-U centers?
Role of spin-orbit coupling unclear
New opportunities for investigating strong electron correlation in controlled environment
Electron Pairing Without Superconductivity
Cheng et al, Nature 521, 196 (2015)

## Slide 30: Correlated Electron Waveguides
Complex oxides add richness to mesoscopic devices

## Slide 31: Electron Waveguides
Analogous to optical cavity modes
Ballistic electron transport
Quantized conductance: Ne2/h
  N= # of quantum channels
Discrete transverse electronic modes
  Tunable by electronic gating
Van Wees et al., PRL 60, 848 (1988).
Quantum Point Contact
Topinka, et al., Science 289, 2323 (2000).

## Slide 32: LaAlO3/SrTiO3 Electron Waveguides

## Slide 33: Landauer Quantization
LB

## Slide 34: LaAlO3/SrTiO3 Electron Waveguides
Parabolic confinement
Kinetic energy
B
LAO
STO
B=6T
z
y
x
Out of plane Magnetic field
Effective frequency
Confining force
Cyclotron frequency

## Slide 35: LaAlO3/SrTiO3 Electron Waveguides

## Slide 36: LaAlO3/SrTiO3 Electron Waveguides

## Slide 37: Avoided Crossings / Re-entrant Pairing
Avoided crossing
  Observed between states with same spin
Re-entrant pairing
  Observed between states with opposite spin
Electron pairing field
  Bp~1-10 Tesla

## Slide 38: Summary
Correlated nanoelectronics
Electron Pairing Without Superconductivity
Correlated electron waveguides
Bp