## Slide 1
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Superconductivity from
Quantum Criticality:
The dome in SrTiO3 and the isotope effect
Yaron Kedem
NORDITA, Stockholm
J. M. Edge, YK, U. Aschauer, N. A. Spaldin,A.V. Balatsky PRL 115, 247002
Multi-Component and Strongly-Correlated Superconductors
Nordita Program 27/07/2016
YK, J.-X. Zhu, A.V. Balatsky
PRB 94, 184507

## Slide 2
Strontium titanate SrTiO3
Wide bandgap insulator (∼3eV )
Small amounts of doping makes it metalic
Perovskyte with antiferrodistortive rotations
SrTiO3
La
Nb
vacancy

## Slide 3
Oldest oxide SC, 1st SC dome
Strontium titanate SrTiO3
Ferroelectric QCP
Many recent interface results:
SC at 100 K in ​FS/​STO
2DEG in LAO/​STO
Ge et. al. Nat. Mat. 14, 285 (2015))
Schooley et. al. PRL 14, 305 (1965)
Cheng et. al. Nature. 521, 196 (2015))
Rowley et. al. Nat. Phys. 10, 10 (2014))
Pre-Pairing and writable SC wires
This talk

## Slide 4
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Outline
Ferroelectric Quantum Critical Point in STO
Quantum model for FE QCP
Effect of doping (explaining the SC dome)
Effect of heavier isotope (Higher Tc, prediction)
Isotope effect and isotope exponent

## Slide 5
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Wang and Itoh, PRB 64, 174104 (2001)
Rowley et. al. Nat. Phys. 10, 10 (2014))
Quantum Paraelectricity in STO
We want a microscopic model for the ferroelectric transition with isotopic mass as tuning parameter

## Slide 6
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Structural Modes in SrTiO3
Antiferrodistortive
rotations
Occur below 110K
Images from Ulrich Aschauer
ETH Zürich/University of Bern
.
Phonon band structure from
Ab initio calculations results
in two Instabilities
Ferroelectric displacement
Do not materialize
(for SrTi16O3)

## Slide 7
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Quantum Ising Model
Excitation (tunneling) energy:
is intersite coupling
Increase M decrease get FE
Curvature
FE
Tunneling
Para
Ferro
Temperature

## Slide 8
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Doping effect on the Instability
Lower barrier: Decrease
→ Enhance tunneling: Increase
→ Mode hardening: Increase
→ The “glue” is lost: Decrease
Mobile electrons screen the repulsion and favor the high symmetry positions.

## Slide 9
Center for Quantum Materials
9
Experiment (Tc)
Theory (⍵ FE)
Edge, YK, Aschauer, Spaldin & Balatsky, PRL 115, 247002 (2015)
due to hardening
Koonce, et al, PR. 163, 380 (1967)
More
carriers
Explaining the dome

## Slide 10
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Phase Diargam

## Slide 11
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Predictions for Isotope replacement
- isotope fraction
Higher Tc for heavier isotopes

## Slide 13
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Calculating Tc
Quantum Ising model:
Modes
At the transition and
Use the MacMillan formula for the coupling constant:
with from above. ( for van Hove singularity at )
Get Tc from solving (numerically):

## Slide 14
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Isotope Exponent
The success of BCS theory: =1/2
The effect is evidence for the important of phonons
Isotope fraction gives an effective mass:
Close to criticality we have

## Slide 15
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Isotope Exponent
Mass tuned QCP implies:
Simple expression for Tc:
Tc is mirror image of : )

## Slide 16
Nordic Institute for Theoretical Physics
Center for Quantum Materials
Conclusions
Developed a model for QCP and SC due to ferroelectric fluctuations
Dependency on doping explain the SC dome in SrTiO3
New prediction: Higher Tc for heavier isotopes
Connection between the critical exponent of the QCP and the isotope exponent of SC