## Slide 1
Experimental searches for electronic hydrodynamics
Andy Mackenzie
Max Planck Institute for Chemical Physics of Solids, Dresden, Germany
School of Physics & Astronomy, University of St Andrews, Scotland
Max Planck Institute
for Chemical Physics of Solids

## Slide 2
Maja Bachmann, Arthur Barnard, David Goldhaber-Gordon, Sean Hartnoll, Seunghyun Khim, Phil King, Markus König, Pallavi Kushwaha, Federico Mazzola, Philip Moll, Joel Moore, Nabhanila Nandi, Thomas Scaffidi, Burkhard Schmidt, Aaron Sharpe and Veronika Sunko
Collaborators
Max Planck Institute for Chemical Physics of Solids, Dresden
University of St Andrews
Stanford University
UC Berkeley
Max Planck Institute
for Chemical Physics of Solids
Notes: Here are my collaborators, mainly from Dresden and St Andrews on the experimental side, but I am also happy to acknowledge some nice discussions that I have had with a number of the people at this meeting.

## Slide 3
Maja Bachmann, Arthur Barnard, David Goldhaber-Gordon, Sean Hartnoll, Seunghyun Khim, Phil King, Markus König, Pallavi Kushwaha, Federico Mazzola, Philip Moll, Joel Moore, Nabhanila Nandi, Thomas Scaffidi, Burkhard Schmidt, Aaron Sharpe and Veronika Sunko
Collaborators
Max Planck Institute for Chemical Physics of Solids, Dresden
University of St Andrews
Stanford University
UC Berkeley
Max Planck Institute
for Chemical Physics of Solids
Notes: Here are my collaborators, mainly from Dresden and St Andrews on the experimental side, but I am also happy to acknowledge some nice discussions that I have had with a number of the people at this meeting.

## Slide 4
Contents
1. Introduction: hydrodynamic flow and challenges for electrons
2. Unusual metal physics of delafossites and a viscous contribution to
transport in zero magnetic field in PdCoO2
4. Conclusions
Max Planck Institute
for Chemical Physics of Solids
3. Electron flow in PdCoO2 in applied magnetic fields; separating
ballistics from hydrodynamics (or trying to!)
Notes: Here are my collaborators, mainly from Dresden and St Andrews on the experimental side, but I am also happy to acknowledge some nice discussions that I have had with a number of the people at this meeting.

## Slide 5
What happens when we drive a classical incompressible fluid through a ‘2D pipe’ by applying a pressure gradient along x?
Fluid flow through an empty 2D channel
x
y
Fluid velocity is greater in the middle of the channel than at the edges
The only transfer of momentum to the outside world is at the edges
We parameterise the strength of the coupling of the fluid to itself along y with the shear viscosity, η. Often this is quoted as a kinematic viscosity ηK = η/ρ where ρ is the density.

## Slide 6
Unlike the fluid in the empty tube, electrons in solids have many ways of making collisions in the bulk that relax the momentum to the solid.
Why is electron hydrodynamics a challenge? Electrons flowing in a standard solid are far from the hydrodynamic regime
W
‘Squalid state physics’ – 99.9999% of materials we work with are so dirty that electronic hydrodynamic corrections are negligible.
In the standard theories of metals they are ignored altogether.

## Slide 7
lMC << W << lMR
lMR << lMC,W
Standard ohmic theory applies;
R is determined entirely by solid resistivity ρ and usual geometrical factors
Hydrodynamic theory applies; R is determined entirely by fluid viscosity η, boundary scattering and ‘Navier-Stokes’ geometrical factors
The 0.00001%
Key point introduced by Gurzhi: In solids, hydrodynamic effects can be parameterised in terms of the relationship between three length scales: momentum relaxing mfp lMR, momentum conserving mfp lMC and sample dimension (here W).
lMR
W
lMC
R.N. Gurzhi, JETP 44, 771 (1963); Usp. Fiz. Nauk 94, 689 (1968)
Pioneering measurements on microfabricated narrow 2DEG channels:
L.W. Molenkamp & M.J.M de Jong , Phys. Rev. B 49, 5038 (1994)

## Slide 8
Can hydrodynamic effects be observed in a true metal?
Looks extremely difficult: Must often work far below TF so lee is very long, and e-e Umklapp is in principle efficient. Expectation is that lMC >> lMR.
Recall hydrodynamic condition:
lMC << W << lMR
However, delafossites seem not to be standard metals.
A site: Pd or Pt
CoO2 octahedra
Non-magnetic low-spin Co3+

## Slide 9
PdCoO2 and PtCoO2: simplicity of electronic structure
Single Fermi surface sheets, experimentally established from angle-resolved photoemssion and de Haas-van Alphen effect measurements.
H.J. Noh et al., Phys. Rev. Lett. 102, 256404 (2009)
C.W. Hicks et al., Phys. Rev. Lett. 109, 116401 (2012)
P. Kushwaha, V. Sunko et al., Science Advances 1, 1500692 (2015)

## Slide 10
PdCoO2 and PtCoO2: record-breaking conductivity

## Slide 11
PdCoO2 and PtCoO2: record-breaking conductivity

## Slide 12
PdCoO2 and PtCoO2: record-breaking conductivity
Carrier concentration of delafossites is about a factor of three smaller than that of monovalent elemental metals

## Slide 13
0
Highest room T relaxation times of any known metals.
PdCoO2 and PtCoO2: record-breaking conductivity

## Slide 14
PdCoO2
Room temperature resistivity about 2.5 μΩcm
Low temperature resistivity a few nΩcm: in-plane mean free paths of tens of microns!
Enormous low temperature conductivity and huge mean free paths
APM, Rep. Prog. Phys. 80, 032501 (2017)
Large anisotropy: resistivity perpendicular to planes approximately 103 higher
Some evidence for phonon drag which could lead to extra momentum-conserving processes

## Slide 15
Clean fabrication - focused ion beam sculpting
300 μm
Focused ion beams can be used to sculpt out arbitrary geometries; beyond a 10-20 nm damage layer this process is clean.
Crystals of PdCoO2 grow 10-20 μm thick

## Slide 16
Clean fabrication - focused ion beam sculpting
Shubnikov-de Haas oscillations from long, narrow meander track of PdCoO2
Our group’s first experiment: Successively narrow the channel in factors of 2, measuring the resistance after every step.
P.J.W. Moll, P. Kushwaha, N. Nandi, B. Schmidt and A.P. Mackenzie, Science 351, 1061 (2016)
Result: Width evolution in zero applied field that matches expectation for significant viscous contribution to flow.
300 μm

## Slide 17
Three limiting regimes to consider
Philosophy of field-dependent measurements: Add a fourth length scale, the cyclotron radius rc = hkF/eB and use it to tune through the above regimes.
Ohmic:
lMR << lMC,W
lMC << W << lMR
Hydrodynamic:
Diffuse-ballistic (like a ‘Knudsen’ regime):
W << lMC, lMR
Lesson learned in the process: The overlap between the three regimes is much broader than it looks when one writes down these neat-looking classifications!

## Slide 18
A blast from the past – transverse electron focusing

## Slide 19
A blast from the past – transverse electron focusing

## Slide 20
A blast from the past – transverse electron focusing

## Slide 21
A blast from the past – transverse electron focusing

## Slide 22
Seen in other famous ultra-high purity materials
Elemental metals and semi-metals (here Bi) in the 1970’s and 1980’s
… and of course graphene
V.S. Tsoi et al., Rev. Mod. Phys. 71 (1991)
e.g. M. Lee et al., Science 353, 6307 (2016)

## Slide 23
First working device in PdCoO2
10 μm contact separation

## Slide 24
Voltage contact 10 μm from current injection point

## Slide 25
Voltage contacts 10 then 20 μm from current injection point
Direct evidence that the ballistic mean free path in this device is greater than 20 μm

## Slide 26
Finer FIB-craft (Maja Bachmann)

## Slide 27
Extremely high resolution data with structure and….
Negative voltage observed at zero applied field

## Slide 28
Negative voltage at zero field significant in hydrodynamic context
Ohmic flow
Viscous flow
L. Levitov and G. Falkovich, Nature Physics 12, 672 (2016)
Negative voltages observed in graphene devices with similar contact spacings (though a slightly different measurement configuration to our usual one).
D. A. Bandurin et al., Science 351, 1055 (2016)

## Slide 29
Explicit measurements in the ‘graphene configuration’
Viscous flow
I
V

## Slide 30
Structure of peaks depends on direction of injection
180 μm

## Slide 31
Ballistic simulations (Aaron Sharpe, Arthur Barnard, David Goldhaber-Gordon) ….

## Slide 32
…. do a very good job of matching the data

## Slide 33
…. do a very good job of matching the data
The simulations also account for the detailed difference of the peak structure for different injection angles.
Excellent agreement from a simulation that includes no hydrodynamics, with a possible exception near zero field.
Experiment
Theory

## Slide 34
The negative voltage at zero field depends on device size
50 x 35 μm
20 x 10 μm
20 x 10 μm
50 x 35 μm
Probably simply a ballistic effect (though not yet understood and hydrodynamic calculations are still desirable).
It would be interesting to know if sample size effects were checked in the graphene experiments.

## Slide 35
Spin-off from analysis of focusing experiments:
directional ballistics
50 x 35 μm
20 x 10 μm
30∘
0∘

## Slide 36
Spin-off from analysis of focusing experiments:
directional ballistics
50 x 35 μm
20 x 10 μm

## Slide 37
Magnetoresistance experiments on simple ‘wires’ at high temperatures (Nabhanila Nandi)
4 μm
7 μm
11 μm
21 μm
Experiment: PdCoO2 at T = 100K
ρxxchannel / ρxxbulk
Navier-Stokes calculation including known W and lMR
Care: kinetic calculations have recently been extended to this regime by Thomas Scaffidi and qualitatively similar predictions are made even if the momemtum-conserving scattering is turned off.
B (T)
B (T)
We may be seeing a hydrodynamic signal but according to our current understanding this is not a definitive experiment.

## Slide 38: Aside: delafossites also host fascinating surface state and magnetic physics leading to fascinating photoemission signals:
Surface states with giant Rashba splitting for transition-metal surface termination in PdCoO2, PtCoO2 and PdRhO2.
For Pd or Pt surface terminations, ferromagnetic surface states are observed.
Sunko, V. et al, 2017, Nature 549, 492
Mazzola F. et al, arXiv:1710.05392
Experiments on bulk spectra from PdCrO2 in which the Cr-O layers are Mott insulating reveal a spectroscopic signal based on a Kondo lattice-like coupling between Mott and free electron layers
Sunko, V. et al, 2018, preprint

## Slide 39
Conclusions
Observation of hydrodynamic electron flow requires such high purity
that it has only very recently become accessible in naturally occurring materials.
2. Extension of electron hydrodynamic theory to include magnetic field
has opened new lines of experimental investigation.
4. A new class of directed ballistics will be enabled by the hexagonal Fermi
Max Planck Institute
for Chemical Physics of Solids
3. Separating hydrodynamic from ballistic contributions is more subtle
than had previously been thought (by me at least).
surfaces of the delafossites.
Notes: Here are my collaborators, mainly from Dresden and St Andrews on the experimental side, but I am also happy to acknowledge some nice discussions that I have had with a number of the people at this meeting.