## Slide 1: Phonons’ Poiseuille flow
Kamran Behnia
ESPCI
Paris

## Slide 2
Benoît Fauqué, Clément Collignon & Alexandre Jaoui
ESPCI, Paris
Valentina Martelli, Juio Larrea & Elisa Saitovitch
CBPF, Rio de Janeiro
Yo Machida & Koichi Izawa
Tokyo Institute of Technology
Alaska Subedi
Ecole Polytechnique
Machida et al. Sci. Adv. 2018
Martelli et al. PRL 2017

## Slide 3: Heat transport in a solid
Thermometers
Resistive wires
Cold finger
sample
Heater
Nodal quasi-particles in superconductors
Neutral excitations in [magnetic] insulators
...

## Slide 4: Outline I. Thermal conductivity of insulators and phonon hydrodynamics II. Observation of the Poiseuille flow of phonons in two solids Black Phosphorus (BP) Strontium titanate (STO) III. A boundary to thermal diffusivity? IV. Electron hydrodynamics and WP2

## Slide 5
The phenomena of thermal conductivity of insulators and the electrical conductivity of metals have specific properties: in both cases the total quasi-particle current turns out to be non-vanishing. ..it follows that when only normal collisions occur in the system, there could exist an undamped current in the absence of an external field which could sustain it.
If collisions are mainly NORMAL (not UMKLAPP), then viscosity sets the flow rate!

## Slide 6: Thermal conductivity of insulators
k = 1/3 C v l
Vandersande & Wood 1986

## Slide 7
Quite successful at high temperature

## Slide 8
Phonon hydrodynamics
A. Cepellotti et al., Nature Comm. 2014

## Slide 9
Thermal conductivity of strontium titanate
Martelli et al. PRL 2017

## Slide 10
Experimental observations of Poiseuille flow
He3 (Thomlinson 1969)
He4 (Mezhov-Deglin 1965)
Bi (Kopylov 1971)
H (Zholonko 2006)
Black P (Machida 2018)
SrTiO3 (Martelli 2018)

## Slide 11: The hydrodynamic regime is fragile!

## Slide 13
Black phosphorus
Machida et al. Sci. Adv. 2018
Three signatures of Poiseuille flow [4K <T<12 K]:
Faster than T3 thermal conductivity
Non-monotonous mean-free-path
Size-dependent Knudsen minimum

## Slide 14
Black phosphorus
Thermal conductivity becomes faster than T3

## Slide 15
The temperature dependence of mean-free-path shows a local peak!
In this hydrodynamic regime :
Momentum-consevering scattering FAVORS the flow!
Hence warming increases the mean-free-path!

## Slide 16
Size dependence of thermal conductivity in black P
Persists beyond ballistic and hydrodynamic limits
Points to ballistic heat carriers even in the umklapp regime!
No superlinear size dependence in the Poiseuille limit.

## Slide 17
The Kundsen minimum is size-dependent!

## Slide 18
Why black P, why Bi? and not Si?
Structural instability
P. A. Littlewood, 1980

## Slide 19
Why black P, why Bi?
Structural instability

## Slide 20: Black P vs. silicon

## Slide 21: Strontium titanate
Antiferrodistortive
Ferroelectric

## Slide 22: Two soft modes

## Slide 23: Ab initio theory: this solid cannot be!
Uschauer and Spaldin, JPCM 2015
Imaginary phonon frequencies!
Owes its very existence to zero-point quantum fluctuations!

## Slide 24
The dielectric coefficient becomes as large as 20000e0!

## Slide 25
Hallmark of Poiseuille flow: faster than T3 thermal conductivity
Martelli et al. PRL 2017

## Slide 26
But specific heat is also faster than T3
Yet, there is a Knudsen minimum followed by a Poiseuille peak!
Martelli et al. PRL 2017

## Slide 27: Non-monotonic temperature dependence of the effective mfp in four solids
Black P
4He

## Slide 29
Revisiting bismuth

## Slide 31
A boundary to thermal diffusivity?

## Slide 32: High temperature

## Slide 34: Specific heat and thermal conductivity

## Slide 35: Extracted thermal diffusivity

## Slide 36: Is there a boundary to thermal diffusivity of insulators?
For all known materials, s>1
Reminiscent of Hartnoll’s boundary for incoherent metals

## Slide 38: Remarks on hydorynamics of electrons

## Slide 39
Changing the sample size by a factor of 75 leads to a thirty percent discrepancy with the expectations of standard theory neglecting momentum-conserving collisions!

## Slide 40
arXiv:1706.05925

## Slide 41
=2.45 10-8W W / K2
Ratio of quanta of charge and entropy!
Why power of two? Because the quanta are present in both force AND flux!
Why p2/3 ? Sommerfeld!
Lorenz number
Sommerfeld number
The Widemann-Franz law

## Slide 42: inelastic scattering
Vertical (small-angle) scattering efficiently decays heat current, but not charge current!
A pondering factor for momentum current:

## Slide 43: i)Electron-phonon scattering
Electric resistivity is expected to vary as T5
Thermal resistivity is expected to vary as T3
As the temperature decreases, the typical wave-vector of phonons decreases.
The relative weight of low-q scattering increases wit decreasing temperature.

## Slide 44: ii)Electron-electron scattering
Electric resistivity is expected to vary as T2
Thermal resistivity is expected to vary as T2
The weight of low-q scattering does not change with temperature!
but

## Slide 45
arXiv:1806.04094

## Slide 46
There is indeed a large finite-temperature deviation!

## Slide 47: Quantifying distinct components
By fitting the data one quantifies :
A2 and A5 in r(T)
B2 and B3 in WT (T)
B2 is almost FIVE times larger than A2

## Slide 48: Quantifying distinct components
The electron-phonon scattering in NOT anomolously enhanced in the thermal channel!
The B3/A5 ratio is similar in WP2 and in Ag!

## Slide 49: Electron-electron (and not electron-phonon) scattering is driving this!
Abundant small-q electron-electron scattering would explain the mismatch!
q
Collision rate
These collisions amplify B2, but not for A2

## Slide 50: What sets the mismatch between T-square prefactors in a given solid?
Material | r0 (nWcm) | A2 (pWcmK-2) | B2(pWcmK-2) | A2/B2
WP2 | 4 | 17 | 76 | 0.22
W | 0.06 | 0.9 | 6.2 | 0.15
Ni | 3 | 25 | 61 | 0.4
UPt3 | 200 | 1.6 106 | 2.4 106 | 0.65
CeRhIn5 | 37 | 2.1 104 | 5.7 104 | 0.4
Herring (1967): The ratio is quasi-universal and of the order of 0.4!
Li & Maslov (unpublished) : No boundary! It can become arbitrarily small!
Theoretical answers:

## Slide 51: What about electron hydroynamics?
T-square electrical resistivity (A2) quantifies momentum-relaxing collisions
T-square thermal resistivity (B2) quantifies momentum-conserving collisions
Comparing their ratio , one can see if there is a hydrodynamic window!

## Slide 52
In 3He:
It arises because of NORMAL scattering and a viscosity which follows T-2

## Slide 53: Putting 3He on Kadowaki-Woods
3He
In our notations, this i

## Slide 54
Is there a hydrodynamic window for electrons?
Momentum-conserving collisions can be quantified thanks to B2T2!

## Slide 55
But, it is extremely fragile!
Residual resistivity , r0 , has a boundary r00 , and an impurity, rimp , component!
If
The window closes!
Future studies on sample with different sizes will tell!

## Slide 56: Summary
Phonon heat flow in Black P becomes hydrodynamic below the peak thermal conductivity
Poiseuille flow requires dominance of normal scattering, favored by proximity to structural instability.
A universal boundary to thermal diffusivity?
The temperature window for electron hydroynamics is linked to the mismatch in T-square resistivity prefactors.