## Slide 1: Detecting axions, and detecting axions with axions
David J. E. Marsh
“Axions in Stockholm”, July 2025
Based on Qiu, DJEM et al (Nature, 2025)

## Slide 2: Outline
Dynamical axion quasiparticles (DAQs)
Detecting quasiparticles with lasers
Detecting axions with axions

## Slide 3: Axion quasiparticles
AQ, also “dynamical axion quasiparticle”, DAQ

## Slide 4
I was 2 weeks old when this came out!

## Slide 5: Topological Insulators
A crystal of Bismuth
e.g. Kane & Mele (2005)
Materials based on Bismuth (e.g. Bi2Se3, Bi2Te3), and Antimony (e.g. Sb2Te3)

## Slide 6: Topological Insulators
Class of materials with insulating bulk and conducting surface.
Surface Hall currents described by electromagnetic Q-term, with Q=p.
e.g. Kane & Mele (2005)
Fig: Wikipedia
Static Q=p (T-symmetry) only affects EM on surface.

## Slide 7
Antiferromagnetic Magnons
Figs: Joel Cramer; Wikiwand.com
A-lattice
B-lattice
Spins have magnetic fields interact via “exchange” with each other, and “anisotropy” to “easy axis” in crystal.
Exchange:
Anisotropy:
External field  spin precession  “spin wave”
Antiferromagnetic “magnetization” below Neel temp TN:

## Slide 8
Antiferromagnetic Magnons
e.g. Haldane (1983), Hofmann (1998)
Mean field theory Heisenberg model in crystal. Use Noether’s theorem.
Magnetic order breaks SO(3) and T  goldstone bosons magnons (spin waves).
(spontaneous) * (explicit) symmetry breaking
“Gell-Mann-Oakes-Renner relation”
Spin wave “stiffness”
“Kittel shift”
Frequency given by exchange, anisotropy and applied fields  O(meV):
Spin wave “mass”
Terms in Lagrangian (and scattering amplitudes!) just like pions and axions:
n live on coset space:
G/H = SO(3)/U(1) = S2

## Slide 9
Fluctuating AFM order couples to E.B  axion ~ magnetoelectric coupling aii.
Need to break T and P symmetries. Original idea: AFM amplitude mode.
Review: Sekine & Nomura (2021)
“Integrate in” dynamics for the order parameter M5 =L=Un ~ q(x,t).

## Slide 10
The amplitude mode is difficult to excite. Need particular symmetries.
New insight: in-plane B tilts spins  effective order parameter fluctuation.
This can be achieved in well understood even-layer MnBi2Te4 “axion insulator”.
Zhu et al (2021); Qiu, DJEM et al (2025)
Experimental measurements
(different set up to main)

## Slide 11: Detecting quasiparticles with lasers

## Slide 12
Su-Yang Xu
Jian-Xiang Qiu

## Slide 13
E-induced magnetization = magnetoelectric effect, a. “Kerr effect”: K rotation of laser ~ magnetization Mz.
Vary E-gate  dK/dE = dM/dE = a.
10 mm
Mapping a on the device
First, measure the static magnetoelectric effect…

## Slide 14
Pump laser, 515 nm, excites the magnon modes  oscillating axion.
Axion-photon coupling causes probe laser polarization angle to oscillate.
a(t) = astat +Da(t)
Now let’s measure the dynamics of a…

## Slide 15
Oscillation Da ~ 0.12 astat.
NB: looks v. low Q resonance. This is optically driven off resonance.
Delay time [ps]
Da [mrad V-1 nm]
Da [e2/2h]

## Slide 16
WE HAVE DISCOVERED THE AXION (QUASIPARTICLE) AND ITS FREQUENCY IS 44 GHZ (0.18 meV)

## Slide 17: Axion quasiparticle parameters
Measurement, plus first principles DFT calculations with VASP (enabled by concrete realization!)
AQ mass
Decay constant (spin wave stiffness)
Refractive index
Resistivity  conductive losses
Magnetic impurity-induced losses
Qiu, DJEM et al (2025)
Schütte-Engel, DJEM et al (2021)
Measured
0.18 meV
DFT
82 eV
DFT
6.4
DFT
0.2 * 10-3
Estimated from dL/L
Micron impurities
0.7 * 10-3
These inferences validate earlier work and provide critical new insights for the future…
Bayrackci et al (2006)

## Slide 18: Detecting axions with axions
See also: DJEM et al (PRL, 2019); Schütte-Engel, DJEM et al (JCAP, 2021)
The idea [formerly?] known as “TOORAD”

## Slide 19: The basic idea
AQ-polaritons give tunable axion DM detector in ~meV. Power estimate: bulk res. with given Q.
Bulk resonance AQ-photon mixing (polariton)  decouple resonant frequency from volume.
“Replace pump laser with axion dark matter, on resonance”
DJEM et al (PRL, 2019)
DM driving force
AQ-photon mass mixing
Diagonalise  “polaritons”
(linear comb. q and E)
c.f. ALPHA

## Slide 20: Computing the sensitivity
Complete treatment: 1d layer model, define “boost factor” b, cf MADMAX.
Include conductance losses for E, Gr, and impurity losses for magnons, Gm.
Schütte-Engel, DJEM et al (2021)
Effective refractive index in polariton material
n goes to zero on res. c.f. Andrew Long’s talk

## Slide 21
Search/engineer materials with lower losses. Coatings/layers to control the refractive index.
The boost factor depends on sample thickness , material losses and refractive index.
B=2 T
Lower: n=3
Upper: n=7
Schütte-Engel, DJEM et al (2021)
Measured+DFT parameters  b2 ~100 in MnBi2Te4.

## Slide 22
Sample size ~ (40cm)2 *(1 mm). Integration per n~1 h, total ~ 3 years. Dark count 10-5 s-1
Propose to grow thick samples of a repeating superlattice of six-layer MnBi2Te4 and spacer layer.
Magnetic tuning 0.1 to 10 T  “rip across frequencies” with current tech (Karl’s dream). Complementary to broad band searches in same range (BRASS/BREAD).

## Slide 23: Comments on the road ahead

## Slide 24
Need to detect the axion polariton in transmission to measure loss parameters.
Schütte-Engel, DJEM et al (2021)
Measuring Polariton Losses

## Slide 25
Low dark count >40 GHz SPDs
Should be possible to scale up these ideas to ~50-100 GHz.
Proof of concept at low AQ-polariton frequencies seems possible.
Paraphrasing Nico Crescini:
“If you build it, they will come”

## Slide 26
meV QCD axion in string theory
meV QCD axion arises at largest h11=491 which likely dominates the set of all Calabi-Yaus.
Currently only good understanding of closed string sector  pre-inflation axions  need to tune qi~p for abundance.
Gendler, DJEM et al (2023)
Axion decay constants strongly correlated with topology:
See Liam’s talk
Unless level crossing is important!
Number of axions, N = h1,1

## Slide 27
Gendler & DJEM (PRL, 2025)
If AQ materials don’t detect the QCD axion, we could falsify parts of the landscape!

## Slide 28
Axion quasiparticles exist. In MnBi2Te4, frequency is 44 GHz.
Mixing with the photon  polariton. Frequency tunable with B.
Predicted losses ~ 10-3  (boost)2 ~ 100.
(40 cm)2 * (1 mm) sample  meV DM detector capable of reaching QCD band.

## Slide 29: Backup slides

## Slide 30
Kerr effect for DM detection
Does not need thick sample (volume independent like NMR). 0.7 nrad/Hz1/2 sensitivity assumed.
Integrate ~3months  not practically tunable. Only depends on magnetic losses.

## Slide 31: Microscopic Theory of AQ
The magnetoelectric coupling a has two contributions: spin and Berry curvature. The spin part comes from the localized magnetic ions; the Berry curvature part comes from the orbital motion of itinerant electrons
Charge density
A topological insulator features Dirac fermions on the top and bottom surfaces, which are gapped by the AFM order, resulting in opposite Berry curvatures on opposite surfaces  real-space dipole, D ~ a.

## Slide 32
Axion Quasiparticles
Axion quasiparticle is the longitudinal (amplitude) magnon mode.
“Integrate in” dynamics for the order parameter M5=Un. Loop  E.B coupling.
“Hubbard-Stratonovich transformation”